## Slide 1: Testing performed on GraphShield 730

## Slide 2: Anticorrosion

## Slide 3: GraphShield 730 Anticorrosion results

## Slide 4: Performance Study
Objective: Evaluate the texture and gloss performance of MicroTex 950 vs. Fluo 750TX in various powder coating systems

## Slide 5: Control Formulas
Resins:
  Epoxy-Polyester Hybrid
  Polyester-TGIC
  Polyester-HAA (Primid)
Each system was evaluated with 1.0% Fluo 750TX vs. 4-5-6% MicroTex 950

## Slide 6: Test Methods Beyond the Visual
Specular Gloss (ASTM D2457)
  60° geometry
Impact Resistance (ASTM D2794) “falling weight test”
  Measures resistance of a paint film from rapid deformation (inch/lb.)
Conical Mandrel Bend (ASTM D522)
  Measure of flexibility (crack resistance) 130°
Crosshatch Adhesion (ASTM D3359)
  Tape test to measure adhesion
Pellet Flow (ASTM D3541)
  Measurement melt flow under low shear

## Slide 7: Visually our best replacement for Fluo 750TX
6.0% MicroTex 950 - Polyester TGIC
6.0% MicroTex 950 - Polyester HAA
1.0% Fluo 750TX Hybrid

## Slide 8: Gloss Efficiency

## Slide 9: Mechanical Properties

## Slide 10: Inclined Plate – Pellet Flow at 15 min/200°C (indication of edge coverage)
#1-4 Hybrid Suitable flow for texture
#5-8 PE/TGIC
Suitable flow for texture
#9-12 PE/HAA
Expand & contract as they shed water during cure
50

## Slide 11: Conclusion
Visually MicroTex 950 is the closest match to Fluo 750TX
Single digit gloss (<6 gloss units/60°)
No negative effect on cross hatch adhesion or mandrel bend
Impact resistance was slightly lower in the polyesters versus the epoxy hybrid
Pellet flow indicates minor restricted flow; good for appearance and edge coverage in texture finishes
We are receiving very positive customer feedback and approvals worldwide
51

## Slide 12: France:Axalta

## Slide 13: USA: Spectra Photopolymer

## Slide 14: Performance Study Overview
Compare the following PropylMatte grades
  PropylMatte 31, PropylMatte 31HD & PropylMatte 31SA
  Clear waterborne 1K polyurethane dispersion
Preparation
  Reichhold Urotuff L63-MPW38
  Level of addition at 4.0% TFW
  #60 rod - 6.0 mil WFT
  S-18 Taber panels
  Dried one week

## Slide 15: Study Overview
Taber Abrasion Analysis
  CS17 wheel
    Produces a harsher abrasion than the smoother CS-10 wheel
  1,000 gram load
  3,000 cycles - 500 cycles
    Check the panels weight
    Repurpose the wheel

## Slide 16: Study Overview
Coefﬁcient of friction (COF)
  Static and kinetic
  200g sliding sled - 0.1 inches/second
  Measured by a force gauge
Measuring gloss of the cured ﬁlm
  60° & 85°

## Slide 17: Coating removed after 2,000 cycles (mg)

## Slide 19: Gloss reduction at4.0% dosage (on TFW)

## Slide 20: Powder Coatings Q-panels
Preferred dark (black) color
  Demonstrates clarity
Common resin systems
  Polyester/TGIC
  Epoxy/Polyester Hybrid
Recommended % dosage
Formulations available upon request

## Slide 21: MP-28AL vs. Polyolefin Wax-PTFE

## Slide 23: 案例

## Slide 24: Performance testing – Coefficient of Friction

## Slide 25: COF Result

## Slide 26: Scratch resistance testing

## Slide 28: Türkiye: Axalta

## Slide 30: Dispersibility of Superslip 6515AL-EZ

## Slide 31: USA:

## Slide 32: Performance Study

## Slide 33: Test Methods

## Slide 35: 案例

## Slide 37: Conclusions
PFAS-free protection in high specification coatings
PolyTuf 1229 provided similar pencil scratch hardness to Polyfluo 190
Superior Taber abrasion performance versus Polyfluo 190 and Polyfluo 900 with only 22.3 mg weight loss after 2,500 cycles

## Slide 38: Industrial Wood finishes

## Slide 39: GI, Protective & Marine

## Slide 40: USA:Carboline (RPM)